## Slide 1: Fibre Amplifiers and Lasers for Near-IR Spectroscopy
Fundamental Principles

## Slide 2: Rare Earth Elements for Near-IR Fibre Amplifiers and Lasers
Rare earth ion | Pump wavelengths (nm) | Emission bands (nm)
Ytterbium, Yb3+ | 915-976 | 1010–1150
Neodymium, Nd3+ | 810, 880 | 860–940, 1040–1080, 1280–1420
Erbium, Er3+ | 980, 1480 | 1500–1620
Thulium, Tm3+ | 790, 1660 | 1700–2100
Holmium, Ho3+ | 1100 | 2000–2200

## Slide 3: Splitting of The Energy Levels of The 4f11 Electrons of Erbium Ions in Glass

## Slide 4: The Most Important Energy Levels for Near-IR Erbium-Doped Fibre Amplifiers and Lasers

## Slide 5: The Einstein Relations for Absorption & Emission Coefficients
where ga(n) and ge(n) are the absorption and emission line shape functions

## Slide 6: Photon and Phonon Interactions with the Energy Levels

## Slide 7: Thermalisation of the Population of the Stark Levels through Phonon Interactions
Photons interact between individual Stark levels, i and j of each manifold, with absorption and emission cross-sections of sij and sji
Thermal population distribution from phonon interactions within Stark levels
Thermal population distribution from phonon interactions within Stark levels

## Slide 8: McCumber Relationship
where se(n) is the effective emission cross-section, sa(n) is the effective absorption cross-section and e is the mean energy difference between the 4I13/2 and the 4I15/2 manifolds
The rapid thermalisation of the Stark energy levels within each manifold through phonon interactions occurs on a timescale much faster than the optical processes. This results in the ‘McCumber relationship’:

## Slide 9: Absorption and Emission Spectrum of Erbium-Doped Fibre
Room Temperature
Room Temperature
Low T
Low Temperature Downward Transitions
Low Temperature Upward Transitions
Low T

## Slide 10: Parameters Describing Erbium-Doped Fibre
Erbium doping density distribution:
Effective area of the doped region:
G is the normalised overlap factor between the erbium density distribution and the optical intensity distribution
Absorption and emission coefficients:

## Slide 11: Erbium-Doped Fibre Amplifier
Atomic rate equation (power expressed in photons/s):
Length averaged fractional inversion level:
Length averaged gain:
t21 is the upper state lifetime
Pump absorption coefficient:

## Slide 12: Typical Gain/Loss Curves for Erbium-Doped Fibre Amplifier for 0-100% Inversion
Fractional Inversion Level,
Gain in dB/m =

## Slide 13: Atomic & Cavity Rate Equations for Fibre Lasers
Atomic rate equation:
Cavity rate equation:
t is the round trip time of the cavity, dq is the number of modes involved, ASE is the amplification factor for the spontaneous emission and RASE is the rate of amplified spontaneous emission.

## Slide 14: Typical Construction of a Ring Cavity Fibre laser

## Slide 15: Typical Parameters for an Erbium Fibre Ring Laser at 1560nm
Lasing wavelength | 1560nm
Absorption coefficient, aa | 1.85dB/m
Emission coefficient, ge | 3.23dB/m
Pump wavelength | 980nm
Pump absorption coefficient, ap | 4.5dB/m
Upper state lifetime, t21 | 10ms
Erbium fibre length, l | 10m
Erbium ion density, re | 5x1024 ions.m-3
Effective area of erbium doping, Se | 10-11 m2
Total length of fibre ring cavity, Lc | 20m
Longitudinal mode spacing, Dnm | 10MHz
Round-trip time of cavity, t | 100ns
Values for cavity loss, ac | 6, 8 or 13dB
Out-coupled ratio of coupler, R | 10%
Erbium fibre output-to-coupler loss, a23 | 3dB

## Slide 16: Typical Output Power Characteristics of Erbium Fibre Ring Laser
Cavity Loss
h is the “slope efficiency”

## Slide 17: Wavelength Tuning, Modulation or Scanning with a FBG and a PZT

## Slide 18: Transient Laser Response after Application of a Step Input to the Pump Power (13dB cavity loss with x = 8)
Delay time
Relaxation oscillations
Delay time to threshold
frequency
decay constant
cavity lifetime

## Slide 19: Example of The Spectral Narrowing Occurring During the Transient Period (1nm Filter Bandwidth)

## Slide 20: The Effect of an Absorption Line of 5GHz Linewidth on The Spectral Narrowing

## Slide 21: Multi-Wavelength Operation of a Fibre Ring Laser
Multi-wavelength outputs generated at the peaks of the Sagnac loop filter through the cavity length modulation induced by the PZT

## Slide 22: Raman Fibre Amplifiers & Lasers
Rayleigh and Raman Scattering

## Slide 23: Raman Fibre Amplifiers & Lasers
Stimulated Raman Scattering (SRS) may be employed to extend the operation wavelength range of fibre lasers and amplifiers.
Raman scattering in optical fibres occurs over a broad frequency band with a broad peak in the Raman gain at a wavelength shift of ~100nm and width of ~5THz.
The Raman gain is given by:
  Ip is the pump intensity in W/m2 and l is the interaction length.
  gR is the Raman gain coefficient with a peak value of ~6x10-14 m/W at a pump wavelength of ~1550nm
Although the Raman gain coefficient is very small, long interaction lengths of several kilometres are possible with optical fibres and high pump intensities can be achieved in the fibre core.

## Slide 24: Summary & Conclusions
The special properties of the 4f electron shell in rare earth elements give rise to the unique characteristics of fibre amplifiers and lasers.
Phonon interactions give rapid thermalisation of the population of the Stark energy levels in rare earth doped fibre, leading to the McCumber relationship between the absorption and emission cross-sections.
The absorption and emission spectra of rare earth doped fibres are broad and predominantly homogeneously-broadened.
Cavity and atomic rate equations provide the basic tools to model the behaviour of fibre lasers under various operating conditions, including steady-state, multi-wavelength, transient and mode-locked regimes.
Stimulated Raman scattering may be employed to extend the operation range of fibre amplifiers and lasers.