## Slide 1: X-Ray Interaction with Matter: Refractive Index and Reflection
David Attwood University of California, Berkeley

## Slide 2: The Equations of Light
Charles-Augustin de Coulomb
Carl Friedrich Gauss
Michael Faraday
André-Marie Ampère
James Clerk Maxwell
Heinrich Hertz
Maxwell’s Equations
Courtesy of Andrew Aquila, AS&T, UC Berkeley, now SLAC/LCLS

## Slide 4: Scattering, refraction, and reflection

## Slide 5: Wave propagation and refractive index at x-ray wavelengths

## Slide 6: Refractive index from the IR to x-ray spectral region

## Slide 7: Refractive index at nanometer wavelengths
Scattering factors courtesy of E. Gullikson, LBL

## Slide 8: Forward scattering and refractive index
Atomic positions and inter-atom electron positions are irrelevant to scattering in the forward direction, simplifying the total current J due to all electrons

## Slide 9: Forward scattering and refractive index (continued)
Move common (r,t) terms to the rhs of the equation
which can be rewritten in the standard form of the wave equation
where the frequency dependent refractive index n(ω) is identified as

## Slide 10: Forward scattering and refractive index (continued)
The square root sign simplifies to
recognizing components of the forward scattering factor we have
which we can write simply as
(3.12)

## Slide 11: Quantum mechanical model of refractive index

## Slide 12: Phase variation and absorption of propagating waves

## Slide 13: Phase shift relative to vacuum propagation

## Slide 14: Mach-Zehnder visible light interferometer
Requires minimal spatial and temporal coherence

## Slide 15: Interferometry with and without background fringes
Attwood 632.8 nm
Attwood 632.8 nm
Flames of small
birthday candles
with and without background fringes
Happy Holidays!
Attwood 632.8 nm

## Slide 16: Phase velocity and group velocity

## Slide 18: Phase velocity and group velocity for a plasma
See Chapter 8, Eqs. (8.113a,b)

## Slide 19: Reflection and refraction at an interface

## Slide 20: Boundary conditions at an interface

## Slide 21: Spatial continuity along the interface

## Slide 22: Total external reflection of x-rays and EUV radiation

## Slide 23: Total external reflection (continued)

## Slide 24: Total external reflection with finite 

## Slide 25: Kirkpatrick-Baez Mirror Pair
Orthogonal mirrors cancel astigmatism
Elliptical surfaces for point to point imaging
Glancing incidence coatings for broad band applications, multilayer coatings for fixed bandpass
Commonly used in synchrotron and FEL beamlines, and in plasma diagnostics. More in Chapter10.
Courtesy of J. Underwood, LBNL

## Slide 26: Reflection at an interface

## Slide 27: Reflection at an interface (continued)

## Slide 28: Reflection at an interface

## Slide 29: Normal incidence reflection at an interface

## Slide 30: Brewster’s angle for x-rays and EUV

## Slide 31: Determining f10 and f20

## Slide 32: Multilayer interference coatings, aka ‘multilayer mirrors’
Recent SXR data courtesy of E. Gullikson, LBNL
W/C, T. Nguyen, UC Berkeley, AS&T
W/C, T. Nguyen, AS&T, UC Berkeley, 1993

## Slide 33: A high quality Mo/Si multilayer mirror

## Slide 34: High reflectivity, thermally and environmentally robust multilayer coating for high throughput EUV lithography

## Slide 35: Multilayer mirrors have achieved a reflectivity of 70%

## Slide 36: High reflectivity multilayer coatings require
Refractive index contrast at the interfaces
Minimal absorption in the low-Z material
Thin high-Z layer where possible G ; DtH /(DtH + DtL)
Interfaces which are chemically stable with time
Minimal interdiffusion at the interfaces
Minimal interfacial roughness (no crystallite formation within the layers, no shadowing in the coating process, surface mobility)
Thermal stability during illumination
Chemically stable vacuum interface(e.g., Si02 or capping layer)
Uniform coating thickness

## Slide 37: Atomic scattering factors for Silicon (Z = 14)

## Slide 38: Atomic scattering factors for Molybdenum (Z = 42)

## Slide 39: Mo/Si multilayer interference coating for EUV lithography
Molybdenum as the “scattering layer”
Silicon as the non-absorbing “spacing layer”
Actually an exaggeration, the complex refractive index of each material plays a role in the reflection process
The absorption edge Si-L3 = 99.2 eV (12.5 nm)
Higher photon energies are absorbed in Si, lower photon energies (longer wavelengths) are not.
Typically l = 13.5 nm for EUV lithography.
Molybdenum has relatively good scattering properties in this photon energy (wavelength) region, with limited absorption.

## Slide 40: Multilayer mirrors satisfy the Bragg condition

## Slide 41: Multilayer mirrors satisfy the Bragg condition

## Slide 42: An angular scan of a multilayer mirror performs a Fourier-transform of the density profile

## Slide 43: High order reflections from a multilayer coating

## Slide 44: Optimized reflectivity with thin “high-Z” layers

## Slide 45: The Borrmann effect in crystals and multilayer mirrors

## Slide 46: Scattering of radiation by a sinusoidal density distribution (atoms or electrons)

## Slide 47: A general scattering diagram

## Slide 48: Sputtered deposition of a multilayer coating
Courtesy of J. Underwood, LBL

## Slide 49: Multilayer coatings measurements at the ALS
Reflectance
World reference standard
Creating uniformity for /50 optics
World record in water window
Wide band, narrow band, and chirped mirrors for fsec applications
Eric Gullikson, Farhad Salmassi, Yanwei Liu (AST, now SLAC), Andy Aquila (AST, now LCLS), Franklin Dollar (UCB EP, now UC Irvine)

## Slide 50: Computed reflectivity of a W/C x-ray multilayer mirror

## Slide 51: Buried, trace amounts of iron in a defective silicon solar cell

## Slide 52: The Cassegrain telescope

## Slide 53: Extreme ultraviolet astronomy

## Slide 54: EUV image of the solar corona showing loops near the solar limb

## Slide 55: Dynamics of the solar corona

## Slide 56: Broad bandwidth mirrors needed for asec/fsec pulses
Multilayer mirrors depend on constructive interference from individual interfaces
Higher reflectivity needs more layers
Bandwidth gets narrower with more layers
Attosecond pulse
Broad bandwidth
Limited number of layers
N<10 layers required for
200 as pulse (@13nm)
∆E(eV) ∙∆τ(fs) ≥ 1.8 fs∙eV (FWHM)
Courtesy of Y.W. Liu, AS&T, UC Berkeley, now SLAC

## Slide 57: More multilayer mirror slides in chapter 10